Mueller® Butterfly Valve Coatings

Standard:	8 Mils nominal interior/exterior of NSF approved 2 part epoxy Ameron, Amercoat 370

Note:  	Above ground valves (those supplied with a handwheel, lever or actuator with position indicator), will have the O.D. coated with (8 mils) Ameron Amercoat 370 (color: Red) as standard, which serves as a suitable topcoat, or as a primer if additional painting is required.

Option:	Holiday Free, Epoxy coat interior 16 mils dry,

Film Thickness (DFT)

input.doc-Rev3/10