## PAINT SYSTEM SUMMARY –

| SYSTEM NO. | A021927A | A021927B | A021927E | A021927C | A021927D6 |
| --- | --- | --- | --- | --- | --- |
| PART NUMBER | 2104972 |  | 2104943 | 2275854 | 2275855 |
| ALTERNATE SYSTEM | NO | NO | NO | NO | NO |
| MULTIPLE COLOR SYSTEM | NO | YES | NO | NO |  |
| MANUFACTURER | PPG PROTECTIVE & MARINE COATINGS | PPG PROTECTIVE & MARINE COATINGS | PPG PROTECTIVE & MARINE COATINGS | PPG PROTECTIVE & MARINE COATINGS | PPG PROTECTIVE & MARINE COATINGS |
| MANUFACTURER'S DESIGNATION | AMERLOCK 400 | AMERLOCK 400 | AMERLOCK 400 | AMERLOCK 400 | AMERLOCK 400B9000 |
| USE CATEGORY | ALL | ALL | ALL | ALL | INT. (F) / EXT. (P) (F) |
| SUBMERSIBLE2 | YES | YES | YES | YES | YES |
| MAT'L CATEGORY | UP/PE | PE | UP/PE | UP/PE | UP/PE |
| MIN. NO. OF COATS | 1 | 2 | 1 | 1 | 1 |
| MINIMUM TOTAL DRY MIL THICKNESS | 4 | 8 | 4 | 4 | 5 |
| NSF/UL RECOAT TIME | 24 HOURS @ 70° F | 24 HOURS @ 70° F | 24 HOURS @ 70° F | 24 HOURS @ 70° F |  |
| NSF/UL CURING TIME | 7 DAYS @ 70° F | 7 DAYS @ 70° F | 7 DAYS @ 70° F | 7 DAYS @ 70° F |  |
| MAXIMUM TOTAL DRY MIL THICKNESS | 8 | 20 | 24 | 24 | 8 |
| COLOR (IF SPECIFIED) | BUFF | BUFF (1ST) WHITE (2ND) | WHITE | RT-1805 BLUE | BLACK |
| SURFACE PREPARATION | SSPC SP-10 | SSPC SP-10 | SSPC SP-10 | SSPC SP-10 | SSPC SP-10 |
| CLASS I INSPECTION | NO | YES | NO | NO | NO |
| AWWA C-550 NSF 61 USDA NFPA CLASS 1 TEMP: 200F | NSF - NO | NSF – NO | NSF – YES | NSF – YES | NSF-NO |

DRN. BY		       CHKD BY

SCALE			       DATE

NOTES:

- AMERLOCK 2 CAN BE USED IN PLACE OF 400 IF NSF IS REQUIRED.

- NSF-61 APPROVED VALVES ARE NOT TO BE USED SUBMERGED IN POTABLE WATER SYSTEMS.

- RECOATING AND CURE TIME FOR POTABLE WATER PER NSF 61.

- 1 PINT OF #861 ACCELERATOR PER 5 GALLONS OF AMERLOCK 400 MAY BE USED.

- MAY BE THINNED WITH THINNER #65 UP TO 12% BY VOLUME.

- ONLY TO BE USED ON MILLIKEN PLANT PRODUCTS.

## PAINT SYSTEM SUMMARY –

| SYSTEM NO. | A021927F | A021927G | A021927H |
| --- | --- | --- | --- |
| PART NUMBER | 2334396 | 2334397 | 2332677 |
| ALTERNATE SYSTEM | NO | NO | NO |
| MULTIPLE COLOR SYSTEM | NO | NO | NO |
| MANUFACTURER | PPG PROTECTIVE & MARINE COATINGS | PPG PROTECTIVE & MARINE COATINGS | PPG PROTECTIVE & MARINE COATINGS |
| MANUFACTURER'S DESIGNATION | AMERLOCK 400 | AMERLOCK 400 | AMERLOCK 400 |
| USE CATEGORY | ALL | ALL | ALL |
| SUBMERSIBLE2 | YES | YES | YES |
| MAT'L CATEGORY | UP/PE | PE | UP/PE |
| MIN. NO. OF COATS | 1 | 1 | 1 |
| MINIMUM TOTAL DRY MIL THICKNESS | 4 | 4 | 4 |
| NSF/UL RECOAT TIME | 24 HOURS @ 70° F | 24 HOURS @ 70° F | 24 HOURS @ 70° F |
| NSF/UL CURING TIME | 7 DAYS @ 70° F | 7 DAYS @ 70° F | 7 DAYS @ 70° F |
| MAXIMUM TOTAL DRY MIL THICKNESS | 24 | 24 | 24 |
| COLOR (IF SPECIFIED) | OXIDE RED | IVORY | MEDIUM GRAY |
| SURFACE PREPARATION | SSPC SP-10 | SSPC SP-10 | SSPC SP-10 |
| CLASS I INSPECTION | NO | NO | NO |
| AWWA C-550 NSF 61 USDA NFPA CLASS 1 TEMP: 200F | NSF - YES | NSF – YES | NSF - YES |

DRN. BY		       CHKD BY

SCALE			       DATE

NOTES:

- AMERLOCK 2 CAN BE USED IN PLACE OF 400 IF NSF IS REQUIRED.

- NSF-61 APPROVED VALVES ARE NOT TO BE USED SUBMERGED IN POTABLE WATER SYSTEMS.

- RECOATING AND CURE TIME FOR POTABLE WATER PER NSF 61.

- 1 PINT OF #861 ACCELERATOR PER 5 GALLONS OF AMERLOCK 400 MAY BE USED.

- MAY BE THINNED WITH THINNER #65 UP TO 12% BY VOLUME.

- ONLY TO BE USED ON MILLIKEN PLANT PRODUCTS.